STANDARD QUALITY ASSURANCE PLAN FOR ELASTOMERIC BEARINGS

| S. No. | Componen t Operation | Characteristic Checks & Tolerances | Frequency & Type of check | Reference Document | Fabriactor control | Inspection details |  | Type of Records | Acceptanc e criteria | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Inspecting Agency | Extent of Inspection |  |  |  |
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 |
| 1.0 | RAW MATERIAL Elastomer | Physical and Chemical Test | As per manufacturer certificate & test required by Authorized inspecting Official of Zonal Railway from Govt./ NABL approved lab | Manufacturer test certificate & Challan | Verification of Reference document. | Authorized inspecting Official from Zonal Railway | From batches at Random and at discretion of Inspecting official | Fabricat ors record. | IRC:83 (Part-II) & referred documents | - The elastomer used in the manufacture of Elastomeric Bearing should be either Natural Rubber (NR) or Chloroprene Rubber (CR) as the raw polymer. - Raw material must meet requirements given in Para 4 (Material) of IRC:83 (Part-II) . |
| 2.0 | Mild Steel | Mechanical & Chemical Test UTS, Yield Stress, Elongation%, Bend test , Impact test at 0 degree centigrade or -20 degree for sub- zero zone, test for C, Mn, Si, P, S etc. | As per Mill TC & test required by Authorized inspecting official of Zonal Railway from Govt. Lab ./ NABL approved lab. | Mill TC and Challan | Verification of Reference document and Complete visual inspection | Authorized Inspecting official of Zonal Railway | One test piece per thickness per heat. / At discretion of Inspecting official | Fabricat ors record Co- related with Mill TC & test report. | IS: 2062, E250 , Quality BO is generally used. However Quality C shall be used for subzero condition. (As specified in approved Drg.). | - Laminates of mild steel conforming to lS: 2062 / lS: 1079 or equivalent international grade shall be used. The yield stress of the material shall not be lesser than 250 Mpa. - Uses of any other materials like fibreglass or similar fabric as laminates are not permitted for the purpose of this Code. - Physical condition of raw material must be visually checked for Pitting, rusting, rolling defect etc before use. - Corrosion protection of exposed steel surfaces, if any, shall conform to the requirement of |

| S. No. | Componen t Operation | Characteristic Checks & Tolerances | Frequency & Type of check | Reference Document | Fabriactor control | Inspection details |  | Type of Records | Acceptanc e criteria | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Inspecting Agency | Extent of Inspection |  |  |  |
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 |
|  |  |  |  |  |  |  |  |  |  | relevant part covering corrosion protection of bearing plates. 5. 100 % Ultra Sonic Testing shall be conducted for 12mm & above thick plates as per provision of relevant specification (IS:4225 or ASTM A435) before processing the material for manufacturing. |
| 3.0 | Manufacturin g Process | Dimension and tolerances. | Visual & Measurement | As per approved drawing | Measurem ent of dimension | Manufactur er inspecting agency | At Discretion of Inspecting official | Fabricat ors record. | IRC 83 Part-II & as per approved drawing | - All Bearing shall conform to the provisions in Clause 6 on Manu- facturing and Workman- ship and Table5: Manufacturing Tolerances of IRC:83 (Part-II) in all respects. - Internal report shall be furnished which will be verified by Zonal Railway Inspector. However random check may be done by Zonal Railway inspector during Manufacturing. - Manufacturing process (any stage) shall be open to inspection by Railway inspecting official. |

| 4.0 | Final inspection (See Note below) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 4.1 | General Inspection | Dimensions of bearing as per specified tolerances. | Visual examination and dimensional check | As per relevant drg. & Specification | Measurem ent of dimension | Authorized inspecting officials from Zonal Railway | 100% | Fabricat ors record & test report. | IRC 83 (Part-II) & referred documents | - All Bearing shall conform to the provisions in Clause 7.9.1.1 of IRC:83 (Part-II) in all respects for Level 1 acceptance testing. - All Bearing shall conform to the provisions in Clause 7.9.2.1 of IRC:83 (Part-II) in all respects for Level 2 acceptance testing. |
| 4.2 | Chemical & Physical Test | Physical and Chemical Test. | As per manufacturer certificate & test required by Authorized inspecting Official of Zonal Railway from Govt./ NABL approved lab | Manufacturer Test Certificate & Challan | Verification of reference document. | Authorized Inspecting Official from Zonal Railway | From batches at Random/ Discretion of Inspecting official | Fabricat ors record. | IRC 83 (Part-II) & referred documents | - Specially moulded test pieces shall conform to the provisions in Clause 7.9.1.2 of IRC: 83 (Part- II) in all respects for Level 1 acceptance testing/ Level 2 acceptance testing. - Ozone resistance test shall be mandatory for all acceptance level. - Test certificate shall be furnished by manufacturers for level I acceptance/ Level II acceptance. |
| 4.3 | Load Test on complete bearings |  |  |  |  |  |  |  |  |  |
| a) | Axial load test | Variation in stiffness | All bearing of the lot shall be tested. | As per relevant drg. and specification | Fabricators record. | Authorized Inspecting Official from Zonal Railway | 100% In case of large lot | Fabricat ors record. | IRC 83 (Part-II) & referred documents | For both Acceptance Level 1 & Acceptance Level 2, all 100% bearings to be checked for axial load tests as per Clause 7.9.1.1 (C) of IRC:83 (Part-II) |
| b) | Shear Modulus | Shear modulus by plotting shear stress strain curve | Load testing on test bearings. | As per relevant drg. and specification | Fabricators record. | Authorized Inspecting Official from Zonal Railway | Mandatory for Large lot and on discretion of Inspecting | Fabricat ors record. | IRC 83 (Part-II) & referred documents | Bearing to be checked as per Clause 7.9.2.3 of IRC:83 (Part-II) |

|  |  |  |  |  |  |  | official for small lot |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| c) | Compressive Stiffness Test | Compressive load deformation curve and compressive stiffness | Load testing on test bearings. | As per relevant drg. and specification | Fabricators record. | Authorized Inspecting Official from Zonal Railway | Mandatory for Large lot and on discretion of Inspecting official for small lot | Fabricat ors record. | IRC 83 (Part-II) & referred documents | Bearing to be checked as per Clause 7.9.2.3 of IRC:83 (Part-II) |
| d) | Shear Bond Test | Required adhesion between elastomer to steel laminate. | Load testing on test bearings for. | As per relevant drg. and specification | Fabricators record. | Authorized Inspecting Official from Zonal Railway | Mandatory for Large lot and on discretion of Inspecting official for small lot | Fabricat ors record. | IRC 83 (Part-II) & referred documents | Bearing to be checked as per Clause 7.9.2.3 of IRC:83 (Part-II) |
| 4.4 | Special Acceptance Inspection |  |  |  |  |  |  |  |  |  |
|  | TGA Method /Any Other Test as per Special Contract Agreement/ As per provisions in Clause 7.9.3 of IRC: 83 (Part-II) | Special type of test (Other than test mentioned in clause 4.3) | As per manufacturer certificate & test required by Authorized inspecting Official of Zonal Railway from Govt./ NABL approved lab | As per special contract agreement | Fabricators record. | Authorized Inspecting Official from Zonal Railway | Discretion of Inspecting official | Test report from Govt./ NABL approve d lab | IRC 83 (Part-II) & referred documents | As per provisions in Clause 7.9.3 of IRC: 83 (Part-II) |

Note:

- For the purpose acceptance testing (Clause 7.9 of IRC:83- Part II), acceptance lots shall be classified as below:

A lot size of 24 or larger number of bearings shall be defined as a large lot and a lot size of less than 24 bearings shall be defined as small lot.

When the number of bearings for a project is large and phased production is permitted, bearing supplied in any one phase will be considered as a large lot.

- The level of acceptance testing shall generally be graded into the following two levels depending on lot size: Level 1 acceptance testing

Level 2 acceptance testing

Acceptance testing level 1 is a higher-level inspection and shall be applicable to large lots. This level of inspection can be specified for small lots also as per the discretion of the Railway. This shall involve manufacture of extra bearings to be used as test bearing and eventually consumed in destructive testing. Acceptance testing level 2 shall be applicable in general for all lots, unless otherwise specified, and shall not involve any destructive testing of finished bearings.